S667 gasket set

Maira ID code: M402367V…..

Technical data:

Material: A2 nitrile rubber

Hardness: 70±5  °shoreA

Traction ressistance:16.5 MPa

Break elongation: minimum 250 %

Work pressure: 350 bar

Work fluid: ET10 oil

Work temperature:-35 oC …+55 oC